**Product Description**

High performance black double sided automotive foam tape, coated with an aggressive solvent acrylic adhesive system meaning this tape is particularly suited to hostile outdoor environments.

**Applications**

Designed for applying to body side mouldings & emblems.

**Features & Benefits**

Good water resistance

UV resistant

Good weather resistance

Easy to use

**Technical Performance**

|  |  |  |  |
| --- | --- | --- | --- |
| Description | Units | Value | Test Method |
| Thickness | mm | 0.80±0.10 | GB/T 7125-1999 |
| Adhesive thickness | MM | 0.95±0.15 | GB/T 7125-1999 |
| Base material | - | Foamed IXPE | - |
| Tack | # | ≥12 | GB/T 4852-2002 |
| Holding strength | Min 70°c-500g-25mm x 25mm | ≥500 | GB/T 4851-1998 |
| 180° Peel strength | N/10mm | ≥8.0 | GB/T 7753-1987 |
| Elongation | % | ≥250 | GB/T 7753-1987 |
| Temperature resistance | °c | -4 to 90 | - |

**Declaration of Conformity Information**

**REACH SVHC Status** – NO SVHC present according to candidates list of the **UK 25/06/20** & **EU 17/01/22**

**RoHS Compliance Status** – Not Applicable

**Storage Details**

Shelf life recommended 1 year from date of despatch at the moderate temperature and humidity environment.